**FORTUS 250MC**

Avoid warping by leaving part in enclosure for >20 minutes.

* ­­ABS shrinks by ~0.1mm after print is complete.
* Do not use 0.1mm clearance (not reliable due to uneven shrinkage)
* Use 0.2mm clearance for (safe) snug fit
* Use 0.4mm for shaft clearances